SECTION 10 26 23

PROTECTIVE WALLCOVERING

PART 1 - GENERAL

1.01	SUMMARY

.	Section includes the following impact and abrasion resistant products:

.	Flexible Protective Wallcoverings

1.02	REFERENCE STANDARDS

.	ASTM D-5420 Impact

B. 	ASTM D-1044 Abrasion

C.  	ASTM D-2197 Hoffman Scratch

D.  	ASTM D-751 Tensile

E.  	ASTM D-1922 Tear

F.  	ASTM D-1308 Stain and Chemical Resistance

1.03	SUBMITTALS

Edit the following paragraph to indicate the correct Division 1 section. Carefully coordinate the statements that follow with Division 1 statements to avoid duplications and conflicts with those provisions specified in Division 1 sections.

.	Submit Samples as requested by the Architect/Designer of all materials specified, in accordance with Section 1.03C.  Do not order materials until approval is received.

.	Manufacturer’s Data: For each type of wallcovering proposed for use on the project, submit copies of reports of tests specified, together with complete description of each wallcovering:  including pattern, total weight, fabric backing, tensile strength, tear strength, abrasion resistance, scratch resistance, impact resistance, stain resistance and fire hazard classification.

.	Submit complete data on each type of adhesive proposed for use.

2.	Manufacturer’s installation instructions

.	Samples: Submit samples, 7 inches wide by 9 inches long, of each material selected.

.	Submit written evidence that all materials proposed for use, conform to recommendations of the protective wallcovering manufacturer for warranted installations.

.	Manufacturer’s Certification:

.	The manufacturer shall provide written certification that the materials shipped to the job site meet all specified physical and performance requirements.  Certification from the dealer or distributor will not be acceptable.  Copies of test reports and corresponding literature shall accompany certification, along with one linear yard samples representing the quality level the contractor proposes to use.

.	Architect/Designer reserves the right to take protective wallcovering samples delivered to the job site, and have them tested at an independent commercial testing laboratory in compliance with the test methods described herein.

1.04	QUALITY ASSURANCE

.	Submittals other than the specified material shall match the appearance and color of the selected material, and equal or exceed the quality, total weight, fabric backing, tensile and tear strength, and fire ratings of the specified product(s).  The decision of the Architect/Designer shall be final.

B.	Imperfections such as engraving roller die marks, roller repeat marks, glossy surface appearance, or other features deemed not in conformance with the specified materials, will be cause for rejection by the Architect/Designer, if evidenced in either the submitted samples, or the manufactured material delivered to the job.

C.	Applicators Qualifications: Work of this section shall be performed by a firm regularly engaged in the installation of vinyl wallcoverings of the types and qualities specified, and acceptable to the Architect/Designer.

1.05	DELIVERY, STORAGE, CONDITIONS

.	Temperatures

.	Maintain substrate surface and ambient temperatures 65°- 80°F at 50% humidity unless required otherwise by manufacturer’s instructions.

.	Do not apply adhesive when substrate surface temperature or ambient temperature is below 65 degrees F.

.	Maintain these conditions six (6) days before, during, and after installation of protective wallcovering.

.	Lighting: Material should be installed under final lighting conditions

- Wall Condition

- The wall surface should be clean, dry, structurally sound, and free of mildew, grease, dust, or other stains.

- Remove any existing wallcovering and adhesive.

- Room humidity should not exceed 50%.

- Wall surfaces should be primed with a high quality acrylic wallcovering primer as approved by manufacturer.  Wall surfaces with significant color variation should be primed with a good quality pigmented wallcovering primer.

1.06	WARRANTY

.	Submit manufacturer’s written five year warranty against manufacturing defects.

.	All wallcovering materials when adhered to a sound surface with the manufacturer’s recommended procedures and adhesive, shall be warranted free of manufacturing defects for a period of 5 years from the date of acceptance of the project.

2.	The foregoing limited warranty is in lieu of all other warranties, expressed or implied, written or oral, including the implied warranties of merchantability and fitness for a particular purpose.  Under no circumstances shall the manufacturer be liable for incidental or consequential damages.

PART 2 – PRODUCTS

2.01	GENERAL

.	After approval of submittals, provide documentation acknowledging the date the material was purchased.  Materials shall be ordered not less than 45 days prior to the scheduled installation date.

2.02	MANUFACTURER

.	All protective wallcovering shall be the product of one distributor.

.	Protective wallcovering shall be __________ as distributed by MDC Interior Solutions, 400 High Grove Blvd., Glendale Heights, IL www.mdcwall.com.

Contact:                                        or 800-621-4006

.	Selections by the Architect/Designer from the manufacturer’s standard color offerings are identified in the finish schedule or design selection summary.

- Substitutions are not permitted.

2.03	MATERIALS

.	Duratec protective wallcoverings: supported vinyl material adhered to a fabric backing.

.	Total Weight: 			38 ounces per linear yard.

2.	Finished Width: 			50” – 52” wide

3.	Thickness:				.030” - .035”

4.	Tensile strength: 			> 200 x 118 (MD x CD)

ASTM D-751

5.	Tear strength:  			 > 3200 x 3200 (MD x CD)

ASTM D-1922

6.	Impact Resistance:			135 (in. /lbs.) cavity breach

ASTM D-5420

7.	Abrasion Resistance: 		Less than .05% (wt. loss %)

ASTM D-1044

8.	Hoffman Scratch			> 2000gms (no image damage)

9.	Stain & Chemical Resistance:	Meet or exceed ASTM D1308.

10. 	Fire Rating:				Pass Class A per ASTM E-84

B.	Adhesive: Roman Pro 774 Heavy Duty Clay Strippable or brands approved as equal by wallcovering manufacturer.

PART 3 – EXECUTION

3.01	INSTALLATION

A.	Contractor shall examine surface for any imperfections; if found shall bring to the attention of the general contractor.

B.	Install wallcovering in accordance with the manufacturer’s written/ printed instructions, using vinyl wallcovering adhesive recommended and approved by the manufacturer.

C.	Before cutting, examine pattern and color and determine that they are the correct pattern and color as specified.

D.	Install each roll in sequence and each strip in the same sequence as cut from the roll.  If pattern is not random, examine for repeat design. If necessary trim selvage deep enough to assure color uniformity.

E.	After the application of three (3) strips, request inspection by the Architect/

Designer, if there are variations in color or pattern, which are considered to be excessive.   The wallcovering distributor shall then be notified for their inspection before any further wallcovering is installed.

F.	The wallcovering shall be smoothed to the hanging surface using a stiff bristled sweep brush or a flexible broad-knife to eliminate air bubbles.

G.	Remove excess adhesive along finished seams immediately after each wallcovering strip is applied.  Use clean warm water, a natural sponge and clean towels.  Change water often to maintain water cleanliness.

3.02	CLEAN-UP COMPLETION

A.	Upon completion of the work, remove surplus materials, rubbish and debris resulting from the wallcovering installation.  Leave areas in neat,

clean and orderly condition.

END OF SECTION